Olefin Metathesis and Rubber Chemistry :

A Powerful Combo in Materials Design

# Prof. Dr. Laurent FONTAINE

Institut des Molécules et des Matériaux du Mans - UMR 6283 CNRS

Université du Maine - Faculté des Sciences et Techniques

Av. Olivier Messiaen - 72085 LE MANS - FRANCE

e-mail : laurent.fontaine@univ-lemans.fr

This presentation will describe our work using olefin metathesis to design and prepare new functional rubber materials based on synthetic 1,4-polybutadiene and natural rubber :

- Bottlebrush copolymers based on a strictly 1,4-polybutadiene trunk by ring-opening metathesis polymerization (ROMP) of cyclobutenyl (macro)monomers using the « grafting through » and « grafting from » strategies ; 1

- Block copolymers based on natural rubber using telechelic cis-1,4-polyisoprene obtained by controlled metathetic degradation of natural rubber and RAFT polymerization.2

Co-workers and students who have been contributing to this work are gratefully acknowledged.

1 F. Leroux, V. Montembault, S. Piogé, G. Brotons, S. Pascual, L. Fontaine, Macromolecules 2016, 49, 4739; F. Leroux, V. Montembault, S. Pascual, L. Fontaine, Macromolecules 2015, 48, 3843; F. Leroux, V. Montembault, S. Pascual, W. Guérin, S. Guillaume, L. Fontaine, Polym. Chem. 2014, 5, 3476; D. Le, G. Morandi S. Legoupy, S. Pascual, V. Montembault, L. Fontaine, Eur. Polym. J. 2013, 49, 972; D. Le, V. Montembault, S. Pascual, F. Collette, V. Héroguez, L. Fontaine, Polym. Chem. 2013, 4, 2168; D. Le, V. Montembault, S. Pascual, S. Legoupy, L. Fontaine, Macromolecules 2012, 45, 7758; G. Morandi, V. Montembault, S. Pascual, S. Legoupy, N. Delorme, L. Fontaine, Macromolecules 2009, 42, 6927; G. Morandi, S. Piogé, S. Pascual, V. Montembault, S. Legoupy, L. Fontaine, Materials Science and Engineering C 2009, 29, 367; S. Piogé, G. Morandi, S. Legoupy, V. Montembault, S. Pascual, L. Fontaine, Macromolecules 2008, 41, 9595; G. Morandi, V. Montembault, S. Pascual, S. Legoupy, L. Fontaine, Macromolecules 2006, 39, 2732.

2 N. Saetung, I. Campistron, S. Pascual, J.-F. Pilard, L. Fontaine, Macromolecules 2011, 44, 784-794; N. Saetung, I. Campistron, S. Pascual, J.C. Soutif, J.-F. Pilard, L. Fontaine, Eur. Polym. J. 2011, 47, 1151.