Feasibility of Manufacturing Cross-laminated Timber Using Fast-grown Small Diameter Eucalyptus lumbers

Chuanshuang Hu, Tu Dengyun, Yuchao Liao, Weiwei Zhang

College of Materials and Energy, South China Agricultural University, Guangzhou, China 510642 Affiliation1     Affiliation2

Abstract

Eucalyptus is one of the most important plantation species in south China. The need of alternate applications of plantation grown hardwood species including eucalyptus is concerned because of the sharp decrease of the demands from pulp and paper industry. The feasibility of manufacturing cross-laminated timber (CLT) using fast-grown small diameter eucalyptus wood (Eucalyptus urophylla × Eucalyptus grandis) was evaluated here. The effects of adhesives, priming treatment, adhesive spread rate, pressure, and pressing time duration on block shear strength (BSS), wood failure percentage (WFP), and rate of delamination (RD) of CLT via block shear tests and cyclic delamination tests.  The results indicated that eucalyptus CLTs made of small diameter lumbers with four types of EP, EPI, PRF, and PUR adhesives could qualified bonding and mechanical requirements according to ANSI/APA PRG 320-2012. The maximum wood failure percentage (WFP) and block shear strength (BSS) values at dry stage condition were 85.2% and 3.51 MPa obtained from specimens bonded with PUR adhesive meanwhile those values at wet stage condition were 58.2% and 1.62 MPa obtained from specimens bonded with EPI and PUR adhesives, respectively. The minimum rate of delamination (RD) value was 7.6%, which was obtained from specimens bonded with PUR adhesive. The optimal pressing parameters were adhesive spread rate 160 g/m2, pressure 0.8 MPa, and pressing time duration 200 minutes when one-component polyurethane adhesive was used to manufacture eucalyptus CLT. The values of MOEs and MORs in the major and minor direction were 11,466 MPa, 24.5 MPa, 681 MPa, and 8.6 MPa, respectively. The values of transverse shear moduli and interlaminar shear strength in the major and minor strength were 91.8 MPa, 1.3 MPa, 241.6 MPa, and 0.5 MPa, respectively. The mechanical properties of eucalyptus CLT were equivalent to those of commercial CLT made of traditional softwoods available in market. Generally, HMR priming treatment was effective to enhance bonding performance and mechanical properties of eucalyptus CLTs. It is safe to conclude that fast-grown small diameter eucalyptus lumber was feasible to manufacture CLT for structural applications.

Introduction

There were several attempts of using hardwoods for structural application because of its higher strength []. The objective of this study was to evaluate the feasibility of manufacturing CLT using fast-grown small diameter Eucalyptus wood (Eucalyptus urophylla × E. grandis).

Materials and method

The Eucalyptus wood (Eucalyptus urophylla × E. grandis) used in this study was a hybrid species grown in Guangxi, China. The scheme of manufacturing eucalyptus CLT was presented in Fig.1.

Fig. 1 The scheme of manufacturing CLT

Results and discussion

Table 1 Mechanical properties of CLT under different bending tests

| Tests | Specimen # | MOE (MPa) | MOR (MPa) | dm (mm) | (kN) | (MPa) | G (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TPB | AE00 | 11466 | 24.5 | 30.21 | 12.6 |  |  |
|  | AE90 | 681 | 8.6 | 124.51 | 4.4 |  |  |
| VSB | AG00 | 10417 |  |  |  |  | 91.8 |
|  | AG90 | 802 |  |  |  |  | 241.6 |
| SSCPB | AS00 | 3546 | 10.8 | 6.94 | 13.5 | 1.3 |  |
|  | AS90 | 573 | 4.2 | 20.88 | 5.2 | 0.5 |  |

Note: 1) dm is the measured deflection center of span, MPa;  is the maximum load, kN;  is the interlaminar shear strength, MPa; G is the transverse shear modulus, MPa.

2) AE00, AG00, AS00 and AE90, AG90, AS90 represent the average values of three replicates in the major and minor strength direction, respectively.

Conclusions

The results obtained via different bending tests indicated that the mechanical properties of fast-grown eucalyptus CLT in this study were equivalent to those of commercial CLT in the market.

References

[1] Frese M, Blaß H J. Characteristic bending strength of beech glulam. Materials and Structures 2007;40(1):3-13.

[2] Castro G, Paganini F. Mixed glued laminated timber of poplar and Eucalyptus grandis clones. Holz als Roh- und Werkstoff 2003;61:291-298.